## Slide 1
Polytechnic School
University of Genoa
Department of Civil, Chemical and Environmental Engineering
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
Supervisors:
Prof. Patrizia Perego
Prof. Jan Oscar Pralits
Dr. Pier Francesco Ferrari
Candidates:
Agnese Gamberini
Chiara Repetto
28th October 2022
Academic year 2021-2022
BIODEGRADABLE ENGINEERED VASCULAR PROSTHESES: A VALIDATION COMPARATIVE STUDY IN BIOREACTOR
Co-supervisor:
Dr. Maria Bolla
1

## Slide 2
VASCULAR PATHOLOGIES
Cardiovascular diseases are the leading cause of death for both sexes
Peripheral arterial disease
Aneurysm
Thrombosis
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
About 17.9 million people died because of CVDs (2019), representing 32% of all global deaths. Of these deaths, 85% were due to heart attack and stroke.
2

## Slide 3
ATHEROSCLEROSIS
It is a pathological condition characterized by alterations of the vessels that lose their elasticity due to the accumulation of calcium, cholesterol, inflammatory cells and fibrotic material
CATHETERIZATION
BALLOON ANGIOPLASTY
USE OF BYPASS
Blood flow
Aterioschlerotic plaque
PROSTHESIS
STRATEGIES
CLASSICAL STRATEGIES
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
3

## Slide 4
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
Dacron (PET)
Teflon (ePTFE)
Polyurethanes
MEDIUM / LARGE CALIBER
Dint>6 mm
Aorta and its ramification
MATERIALS
Dint<6 mm
Blood vessels of the lower and upper limbs
PCL+PGS (mixture)
Difficulties in design
Lack of vascularization
and thrombogenic risk
VASCULAR SUBSTITUTES
SMALL CALIBER
INNOVATIVE APPROACH
4

## Slide 5
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
The current challenge lies in producing prostheses on which
cells can grow, completely regenerating the new vessel
Engineered prostheses with bioactive compounds that can overcome the problems that common vascular scaffolds show in vivo.
VASCULAR TISSUE ENGINEERING
5

## Slide 6
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
OBJECTIVE
The main objective of this work is to fabricate an engineered vascular prosthesis
STEP 1
STEP 2
Study the behavior of the vascular electrospun prostheses and approach in conditions similar to physiological and pathological ones
REQUIREMENTS
Home-made bioreactor
High-performance bioreactor
Biological | Mechanical | Additional
Biocompatible | High flexibility | Small caliber
Biodegradable | Porosity | Functionalized with bioactive compounds
Inert, non-toxic | Suturable | Approved materials (FDA)
6

## Slide 7
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
MATERIALS AND METHODS
PREPARATION OF POLYMER SOLUTION
PCL
PGS
QUERCETIN+ETHANOL
20% (m/v)
20% (m/v)
0.05% (m/v)
ratio 9:1 (v/v)
1:1
CHLOROFORM:ETHANOL
7
Poly(caprolactone)
Poly(glycerol sebacate)

## Slide 8
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
MATERIALS AND METHODS
ELECTROSPINNING
Polymeric solution passes through a capillary, in an electric field and electrospun on a rotating collector which has a diameter of
2 mm or 5 mm
PARAMETER | DIAMETER (2 mm) | DIAMETER (5 mm)
V (volume) | 1.5 mL | 2 mL
R (rate) | 2.20 mL/h | 1.1 mL/h
D (needle-collector distance) | 18 cm | 18 cm
V (voltage) | 17.0 kV | 17.0 kV
vr (rotation speed) | 500 rpm | 500 rpm
vt (translation speed) | 600 mm/min | 600 mm/min
t (time) | 40 min | 1.50 h
8

## Slide 9
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
MATERIALS AND METHODS
GELATIN COATING
Mechanical stirrer
Becker with water
Collector
Heating and magnetic stirrer
Prosthesis
Gelatin
To reduce the porosity and permeability of the construct, preventing possible blood leakage
T = 37°C
V = 135 rpm
t = 1h
- Sterilization under UV rays
- t = 1h
9

## Slide 10
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
MATERIALS AND METHODS
BURST PRESSURE TEST
Prostheses were connected to a pump working with water that increases water pressure since it achieves a maximum pressure value
SAMPLE | PRESSURE (mmHg) | PERMEABILITY (%)
PCL:PGS 1:1 | 150 | 100
PCL:PGS 1:1 + G + Q | 150 | 0
 | 225 | 100
To understand the maximum working pressure that the prosthesis can tolerate
10

## Slide 11
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
MATERIALS AND METHODS
Chamber containing the prosthesis
Flow rate was constant
Phosphate Buffered Saline
Samples were collected to determine the release of gelatin and quercetine
HOMEMADE BIOREACTOR
80 mmHg
120 mmHg
80-120 mmHg
Peristaltic pump
Reservoir
Pressure gauge
T = 37°C
28th October 2022
11

## Slide 12
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
MATERIALS AND METHODS
HIGH-PERFORMANCE BIOREACTOR
Peristaltic
pump
Chamber containing
the prostheses
Reservoir
Compliance chamber
Damper
80-120 mmHg
T = 37°C
Flow rate was constant
Phosphate Buffered Saline
Samples were collected to determine the release of gelatin and quercetine
12

## Slide 13
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
13

## Slide 14
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
MATERIALS AND METHODS
MORPHOLOGY
Dimensional analysis of the fibers through the ImageJ software
MECHANICAL ANALYSIS
Allows vertical elongation of the prosthesis until failure in the uniaxial direction
Scanning electron microscopy (SEM) analysis
14

## Slide 15
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
MATERIALS AND METHODS
RELEASE OF GELATIN
RELEASE OF QUERCETIN
Spectrophotometric analysis
Abs (λ) = 562 nm
Bicinchoninic acid assay (BCA)
Spectrophotometric analysis Abs (λ) = 370 nm
Chart: Quercetin spectrum
28th October 2022
15

## Slide 16
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
MATERIALS AND METHODS
STEADY STATE
< 2000
Flow is laminar
Hp of Newtonian fluid
Constant pressure gradient
Poiseuille flow
16

## Slide 17
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
RESULTS AND DISCUSSION
Morphology
Mechanical analysis
PRESSURE (mmHg) | YOUNG’S MODULUS (MPa) | TENSILE STRENGTH (MPa) | ELONGATION (%)
80 mmHg | 2.11 ± 1.60 | 1.01 ± 0.29 | 87.55 ± 28.52
120 mmHg | 4.02 ± 0.32 | 1.22 ± 0.29 | 89.44 ± 16.52
80-120 mmHg | 2.86 ± 1.30 | 1.36 ± 0.39 | 91.88 ± 30.58
80-120 mmHg (HPB) | 4.66 ± 1.85 | 1.39 ± 0.92 | 50.54 ± 23.26
Human artery | 2.58 ± 0.34 | 1.13 ± 0.06 | 46.54 ± 11.31
Similar values
Possible future in vivo applications
Internal surface of the control sample
External surface of the control sample
Inner surface (PCL: PGS + gelatin+ quercetin),
External surface (PCL: PGS + gelatin + quercetin).
PRESSURE | FIBER DIAMETER (µm)
80 mmHg | 4.589 ± 0.53
80-120 mmHg | 4.572 ± 0.91
120 mmHg | 4.524 ± 0.15
Control Sample (PCL:PGS) | 3.46 ± 0.48
17
HPB: high performance bioreactor

## Slide 18
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
RESULTS AND DISCUSSION
DEGRADATION
Chart: SHEAR STRESS ON THE PROSTHESIS WALL
| 0.106 | 0.109
0,106 0,109 | 80 | 120
Pressure | Degradation (%) | Fluid uptake (%)
80 mmHg | 28.75 ± 3.18 | 285.45 ± 12.98
120 mmHg | 29.13 ± 4.41 | 279.58 ± 39.85
80-120 mmHg | 40.62 ± 26.11 | 228.68 ± 3.05
80-120 mmHg (HPB) | 33.76 ± 2.60 | 240.32 ± 20.16
Prosthesis | Degradation (%) | Fluid uptake (%)
PCL:PGS | 35.00 ± 3.70 | 164.40 ± 41.97
With quercetin | 32.51 ± 2.53 | 274.19 ± 27.61
18

## Slide 19
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
RESULTS AND DISCUSSION
RELEASE OF GELATIN
Chart: RELEASE RATE OF gelatin IN THE HOME-MADE BIOREACTOR
| 0 | 0.02 | 0.04 | 0.08 | 1 | 2 | 3 | 4 | 5
120mmHg | 0 | 59.6662 | 174.366 | 271.9258 | 271.9258 | 274.7127 | 269.0425 | 271.2331 | 270.489
80mmHg | 0 | 10.087 | 37.4635 | 37.9913 | 39.4608 | 41.3094 | 44.412
19
Chart: RELEASE RATE OF gelatin IN THE HOME-MADE BIOREACTOR
| 0 | 0.02 | 0.04 | 0.08 | 1 | 2 | 3 | 4
80-120mmHg | 0 | 56.8403 | 94.4423 | 278.9545 | 288.2505 | 280.3628 | 278.1067 | 278.369
Chart: RELEASE RATE OF gelatin IN THE HIGH PERFORMANCE BIOREACTOR
| 0 | 0.02 | 0.04 | 0.08 | 1 | 2 | 3 | 4 | 5
80-120mmHg | 0 | 185.342 | 221.1101 | 383.8176 | 396.6748 | 387.4587 | 385.0705 | 385.4524 | 385.5396

## Slide 20
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
Chart: DERIVATIVE OF THE RELEASE OF GELATIN IN THE HOME-MADE BIOREACTOR
| 0.02 | 0.04 | 0.08 | 1 | 2 | 3 | 4 | 5
120mmHg | 69.6859 | 91.7608 | 94.4965 | 3.3442 | 0.21423 | -2.6746 | 1.1783 | -1.3719
80mmHg | 10.087 | 27.3764 | 0.52781 | 1.4695 | 1.8486
Chart: DERIVATIVE OF THE RELEASE OF GELATIN IN THE HOME-MADE BIOREACTOR
| 0.02 | 0.04 | 0.08 | 1 | 2 | 3 | 4 | 5
80-120mmHg | 65.1477 | 114.9922 | 166.3671 | 11.1209 | -3.3317 | -0.11368 | -6.5585 | 3.5328
Chart: DERIVATIVE OF THE RELEASE OF GELATIN IN THE HIGH PERFORMANCE BIOREACTOR
| 0.02 | 0.04 | 0.08 | 1 | 2 | 3 | 4 | 5
80-120mmHg | 180.0557 | 13.8898 | 83.4849 | 7.6722 | 4.3888 | -7.9655 | -1.7137 | -0.19498
RESULTS AND DISCUSSION
RELEASE OF GELATIN
28th October 2022
20

## Slide 21
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
RESULTS AND DISCUSSION
RELEASE OF QUERCETIN
Chart: RELEASE OF QUERCETIN IN THE HOME-MADE BIOREACTOR
| 0 | 0.02 | 0.04 | 0.08 | 1 | 2 | 3 | 4 | 5
120mmHg | 0 | 6.1585 | 9.1653 | 8.616 | 8.517 | 8.5427 | 8.6521 | 8.6056 | 8.4913
80mmHg | 0 | 3.8495 | 3.2524 | 3.3508 | 4.1673 | 2.123
Chart: RELEASE RATE OF QUERCETINE IN THE HIGH PERFORMANCE BIOREACTOR
| 0 | 0.02 | 0.04 | 0.08 | 1 | 2 | 3 | 4 | 5
80-120mmHg | 0 | 7.8775 | 6.5098 | 4.9314 | 4.9042 | 4.9009 | 4.9256 | 4.9032 | 4.905
Chart: RELEASE RATE OF QUERCETIN IN THE HOME-MADE BIOREACTOR
| 0 | 0.02 | 0.04 | 0.08 | 1 | 2 | 3 | 4 | 5
80-120mmHg | 0 | 0.13145 | 0.10419 | 0.14092 | 0.15866 | 0.1518 | 0.14979 | 0.14794 | 0.16552
21

## Slide 22
28th October 2022
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
RESULTS AND DISCUSSION
RELEASE OF QUERCETIN
Chart: DERIVATIVE OF THE RELEASE OF QUERCETIN IN THE HOME-MADE BIOREACTOR
| 0.02 | 0.04 | 0.08 | 1 | 2 | 3 | 4 | 5
120mmHg | 6.1585 | 3.0067 | -0.54928 | 0.013564 | -0.082289 | 0.10939 | -0.046559 | -0.11423
80mmHg | 422.3094 | 402.4923 | 5.8695 | 11.6579 | 18.3836
Chart: DERIVATIVE OF THE RELEASE OF QUERCETIN IN THE HOME-MADE BIOREACTOR
| 0.02 | 0.04 | 0.08 | 1 | 2 | 3 | 4 | 5
80-120mmHg | 0.13145 | -0.027259 | 0.036724 | 0.017745 | -0.0068602 | -0.0020142 | -0.0018476 | 0.0034225
Chart: DERIVATIVE OF THE RELEASE OF QUERCETIN IN THE HIGH PERFORMANCE BIOREACTOR
| 0.02 | 0.04 | 0.08 | 1 | 2 | 3 | 4 | 5
80-120mmHg | 7.8775 | -1.3677 | -1.5784 | -0.027226 | -0.0033038 | 0.024707 | -0.022385 | 0.0017994
22

## Slide 23
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
In the future:
Dynamic conditions
Non-Newtonian fluid
In the presence of vessel cells in bioreactor
CONCLUSIONS and FUTURE PERSPECTIVES
SEM  Micrometric fibers are randomly electrospun
Release of the biomolecule  Adequate to the objectives
Degradation and mechanical properties  Consistent with the behavior that the prostheses could have once implanted
In both bioreactors, the results obtained have almost similar trends
But high-performance bioreactor:
Optimize the processes
Simpler process for the operators
Similar to be applied in vivo application
28th October 2022
23

## Slide 24
Agnese Gamberini, Chiara Repetto
Biodegradable engineered vascular prostheses: a validation comparative study in bioreactor
MASTER DEGREE IN CHEMICAL AND PROCESS ENGINEERING
THANKS FOR YOUR ATTENTION!
24